## Slide 1: RAVENOL SWT
www.ravenol.de
ISO 150 | 220 | 320 | 460 | 680
Synthetic Wind Turbine – Technical Report

## Slide 2: RAVENOL SWT | APPROVALS
www.ravenol.de
Mastering the most extreme demands across the entire application range – RAVENOL targets a Multi-Specialist-Approach with SWT that far exceeds every single standard.
Approval | Ravenol SWT 150 | Ravenol SWT 220 | Ravenol SWT 320 | Ravenol SWT 460 | Ravenol SWT 680
Eickhoff Gearboxes QSV19.0002 | • | • | • | • | •
FLENDER AS 7300 | • | • | • | • | •
Renk 36011-11 | • | • | • | • | •
Renk Augsburg ZAN 36011 | • | • | • | • | •
SEW gear units: IGP, XP, P-X-Series | • | • | • | • | •
SEW gear units: R-, K7-, F-, IG X-Series | • | • | • | • | •
Sumitomo/Hansen HP1 | • | • | • | • | 
Sumitomo/Hansen HP2 | • | • | • | • | 
Sumitomo/Hansen HPP | • | • | • | • | 
Sumitomo/Hansen M4ACC | • | • | • | • | 
Sumitomo/Hansen M5CT | • | • | • | • | 
Sumitomo/Hansen P4 | • | • | • | • | 
Sumitomo/Hansen Paramax® | • | • | • | • | 
ZF Industrieantriebe Witten ZN-WN-145 | • | • | • | • | 
ZF TE-ML | 27D | 27F | 27H | 27J | 

## Slide 3: RAVENOL SWT | BEARING PROTECTION
RAVENOL SWT provides advanced bearing protection
Passes a wide range of demanding tests, far beyond typical gearbox operating conditions
DIN 51819-3 | FE-8 Test Rig
WEC Test FVA 707 V
Schaeffler / FAG 4-step test
0
20
40
60
80
100
120
140
Wear mass [mg]
 | 117,7 mg | 
permissible limit 30 mg |  | 
1 mg |  | 
SWT
Competitor
0
5
10
15
20
25
30
35
Step 1
Step 2
Step 3
Step 4
Wear mass [mg]
permissible limit 30 mg
No WEC (White Etching Cracks) Damages after 1750h -> no WEC propagation with SWT!
www.ravenol.de

## Slide 4: RAVENOL SWT | BEARING PROTECTION
RAVENOL SWT stabilizes the wear rates of rolling bearings
Test according to DIN 5119-3 mw50 (80h) on the FE8 test rig with a competitor lubricant
Replacement of the lubricant with RAVENOL SWT and repeat of the test (80h) with the used rolling bearings
Wear-related gearbox problems can be completely stopped by using RAVENOL SWT; excessive wear rates are stabilized
0
70
80
90
Kompe�tor 63 mg
10 20 30 40 50 60
Wear mass [mg]
permissible limit 30 mg
0
10
80
90
20 30 40 50 60 70
new wear in the second run [mg]
 |  |  |  | SWT 0mg |  |  |  |  |  | 
www.ravenol.de

## Slide 5: RAVENOL SWT | GEAR PROTECTION
Initial condition
After test completion – like new
0 2 4 6 8 10 12 14 16 18 20
FZG load stage
RAVENOL SWT provides outstanding protection for gear teeth
FZG A/16.6/90 test with RAVENOL SWT
The highest measurable load stage (14) was passed without any signs of wear
permissible limit at load stage 12
www.ravenol.de

## Slide 6: RAVENOL SWT | GEAR PROTECTION
RAVENOL SWT protects gear teeth in all operating conditions
Very good performance at low speeds
Low rotational speed at high torque
Very low wear mass
Excellent protection against shock and impact loads
Maximum loading of the test gearbox
No time for the test gear teeth to run-in
The maximum load stage 12 was exceeded
0
5
25
30
Stage 1
Stage 2
Stage 3
Stage 4
Stage 5
10 15 20
Wear mass [mg]
FZG Test C/0.05/90/12
permissible limit
www.ravenol.de

## Slide 7: RAVENOL SWT | FOAMING BEHAVIOR
The formulation of RAVENOL SWT impresses with its very low foaming tendency
0
250
500
750
Foam volume [ml]
ASTM D892 foam test after 5 minutes
ISO 150
SWT with defoamer
ISO 320
SWT without defoamer
ISO 680
Competitor VG 320
permissible limit |  | 
www.ravenol.de

## Slide 8: RAVENOL SWT | FOAMING BEHAVIOR
The formulation of RAVENOL SWT impresses with its very low foaming tendency
Foaming behavior and air-release capability often represent an optimization challenge
Despite its very good foaming characteristics, SWT is able to release large amounts of air in a short time
ASTM D3427 air release at 50°C (ISO 320)
SWT
Competitor
44 min
5:50 min
ASTM D3427 air release at 75°C (ISO 320)
0
5
15
20
10
Time [min]
SWT
Competitors
www.ravenol.de

## Slide 9: RAVENOL SWT | ELASTOMER COMPATIBILITY AND FILTERABILITY
12
10
8
6
4
2
0
-2
-4
Volume change [%]
SWT is characterized by its compatibility with static and dynamic seals
Protects seals from common failure mechanisms
Robust, passed NBR902, FKM585 & FKM260466
Static and radial shaft-seal tests according to Flender test conditions
Unlike many competitors, it does not cause excessive swelling of nitrile rubbers, which can be susceptible to it
NBR902 volume change
Competitors
SWT
permissible limit −2%
 |  |  |  | permissible |  |  |  | 
 |  |  |  |  |  | limit 5% |  | 
SWT demonstrates fine filtration properties
Longer oil change intervals require increased use of finer filtration to ensure oil cleanliness and component protection.
Filter blockages or the removal of additives can lead to foaming, increased friction, and wear.
Important filter designs typically have pore sizes of ≥ 3 µm to ensure a good balance between filtration efficiency and additive retention.
Internal standards: Hydac and CC Jensen:
No loss of additive chemistry
Passing of the Flender foam test
after filtration
www.ravenol.de